## Slide 1: Restoration of five semi-leather bindings of books of the 19th century from the collection of the D.I. Mendeleev St. Petersburg State University
Final qualifying work
4th year student
Isilyaev Igor Vladimirovich
Scientific adviser:
Associate Professor, PhD in Art History
Torbik Vladimir Sergeevich
Saint Petersburg 2023

## Slide 2: Историческая справка
Museum-archive of D.I. Mendeleev St. Petersburg State University
Museum-archive of the great
Russian scientist
Dmitri Ivanovich Mendeleev
located in the main building
twelve colleges
St. Petersburg
state university.

## Slide 3: Историческая справка
In the office
collected an extensive library.
The bulk of the books
received in the 80-90s of the 19th century.
Museum-archive of D.I. Mendeleev St. Petersburg State University
At present, the total number of books, brochures and individual prints reaches
16,000 units.

## Slide 4: The result of the inspection of the condition of the bindings
Damage form
2% Old restoration
40% Deformation of the book binding
100%!!! Increased acidity of paper Drip method (LKRDrN-meter-340) pH=6.1
10% sewing damage
20% Damage to notebooks
25% Cover Damage
30% Destruction of the spine, separation from the binding

## Slide 5: State of the binding before restoration
Convolute:
Баконъ, Баконъ. Собранiе сочинiй
1874, 316 Д.М.
Date of execution:
end of the 19th century. 1874
Inventory number: ММ ВХ ЭФЗК 2607
1. the sewing cords are torn

## Slide 6: State of the binding before restoration
Convolute:
G.Herrm.Oelsner. Доливо-Добровольская
В.А., Забудский Н. 1892 Технологiя Баллистика Удобрения 333 Д.И,
Date of execution:
end of the 19th century. 1890-1892
Inventory number: ММ ВХ ЭФЗК 1665
2. the leather spine is torn off

## Slide 7: State of the binding before restoration
Convolute:
Алексеев В.,Забудский А.,Frenkel M. Алексеевъ, Калкутскиiй, Петрушевский и др. 1890. 241 Д.М.
Date of execution:
end of the 19th century. 1886-1890
Inventory number: ММ ВХ ЭФЗК 2454
3.Deformed cardboard cover

## Slide 8: State of the binding before restoration
Convolute:
Winkler C., Efimov A.I., Kapustin S.Ya., Aristov N. Mixture.. 1890. 243 D.M.
Execution date:
end of the 19th century, 1866-1890
Stock No.: MM VX EFZK 2487
4.
Damage: Notebooks fall out of the book block.

## Slide 9: State of the binding before restoration
Book:
Gerard, Chancel, Mendeleev D.I. 1007.
Analytical Chemistry of Gerard and Chancel. Qualitative analysis.
383 D.M.
Execution date:
Late 19th century, 1864
Stock No.: MM VX EFZK 1071
5.
Damage: according to the initial visual examination, there is no original marbled paper.

## Slide 10: Restoration process
Disassembly of the binding: the covers are separated, the exact dimensions of the cardboard covers and corners are removed.
Cardboard lids. Marble

## Slide 11: Restoration process
Soaking in a ditch. Department of marble and endpapers. Transfer for restoration.
Marble. Bookends.

## Slide 12: Restoration process
Pressing the marble paper between the cloth until completely dry.
Marble.

## Slide 13: Restoration process
Deformed block. The formation of the spine in a vise. Removing adhesive residue.
Book block

## Slide 14: Restoration process
Materials: natural linen thread, needle.
On the book block
are recovering
sewing cords
Restoration process

## Slide 15: Restoration process
Before restoration After restoration and filing to the block
Restoration and filing of the first notebooks

## Slide 16: Restoration process
Destruction of sewing before restoration Restoration of sewing after restoration
Filing of notebooks of the book block.

## Slide 17: Restoration process
Combing yarn cords sewing into fibers
Manufacturing and
gluing
paper sleeve
book block
clamped down to
complete drying
Book block. The final stage: the formation of the "mushroom cap"

## Slide 18: Restoration process
Vegetable tanned calfskin leather. Material: aniline dye.
Toning the new leather base

## Slide 19: Restoration process
Production of new cardboard covers Production of leather corners

## Slide 20: Restoration process
Cleaning a fragment of the old spine from traces of paper lag and glue

## Slide 21: Restoration process
Marking bandages on a new lag Gluing leather strips - Oblique cut edges
binding bandages
Imitation of "false" sewing bandages on a new lagging

## Slide 22: Restoration process
Spine recovery
The new leather base is lagged glued.
We select "false" bandages
3. Glue the old spine
on a new leather base.
2. We fix the adhesive with elastic
rubber bandages.
We make a binding through
end hinges of covers.
select "ears"

## Slide 23: Restoration process
New corners New spine Old fragment on a new basis
Binding assembly

## Slide 24: Restoration process
1. Bonding of the marbled paper 2. Cords glued on the inside to the lids
Marble paper and cords

## Slide 25: Restoration process
Materials: flour glue, cloth, Japanese paper, small weight.
Strengthening gaps on endpapers.

## Slide 26: Restoration process
Upper binding cover Lower binding cover
Pasting bookends

## Slide 27: Restoration process
Marble tinting
paper on the ends of the lids
Reinforcing the front
marble paper (PVButyral
5% alcohol solution)
Processing of leather elements
lanolin-based impregnation
and wax

## Slide 28: The result of restoration activities
Before restoration After restoration
D.M. 316
1.Repaired sewing cords;
2. Notebooks are filed,
formed, fortified
book block;
3. Made new carton
Covers;
4. New corners were made and
a new spine for the old base;
5.Reinforced marble paper.

## Slide 29: The result of restoration activities
Before restoration After restoration
D.M. 243
1.Repaired sewing cords;
2. Notebooks are filed,
formed, fortified
book block;
3. Made new
cardboard covers;
4. Made new corners and a new spine
for the old base;
5.Refurbished
marble paper.

## Slide 30: The result of restoration activities
Before restoration After restoration
D.M. 383
1.Repaired sewing cords;
2. Notebooks are filed,
formed, fortified
book block;
3. Made new carton
Covers;
4. New corners were made and
a new spine for the old base;
5. Restored marble paper.

## Slide 31: The result of restoration activities
D.M. 333 Before restoration After restoration

## Slide 32: The result of restoration activities
D.M. 241 Before and after restoration ("head") Before and after restoration ("tail")

## Slide 33: Conclusion
In the restoration of semi-leather bindings from the collection of the D.I. Mendeleev
an alternative technique was used to restore the basic functions of the binding
accepted in many restoration centers, laboratories and libraries in Russia.
Reversible adhesives were used: flour and animal origin, neutral cardboard,
vegetable tanned calfskin, linen, aniline dyes.
The binding has gained strength and high performance characteristics.
All this makes it possible to use bindings in the museum exposition and
in scientific works.
Photo: 1.2; https://spbu.ru/news-events/krupnym-planom/muzey-arhiv-d-i-mendeleeva-spbgu-svyaz-vremen